| 1. Report No. FHWA/LA/08-437 | 2. Government Accession No. | 3. Recipient’s Catalog No. |
| --- | --- | --- |
| 4.Title and Subtitle STRUCTURAL MONITORING OF RIGOLETS PASS BRIDGE | 5.Report Date December 2008 |
|  | 6.Performing Organization Code |
| 7.Author(s) Robert N. Bruce, Jr., John J. Roller, and Henry G. Russell | 8.Performing Organization Report No. |
| 9.Performing Organization Name and Address Tulane University 6823 St. Charles Avenue New Orleans, LA 70118 | 10. Work Unit No. |
|  | 11. Contract or Grant No. LTRC Project No. 04-2ST State Project No. 736-99-1215 |
| Sponsoring Agency Name and Address Louisiana Department of Transportation and Development Louisiana Transportation Research Center 4101 Gourrier Avenue Baton Rouge, LA 70808 | 13. Type of Report and Period Covered Final Report April1, 2005 – April 30, 2009 |
|  | 14.Sponsoring Agency Code |
| 15.Supplementary Notes Conducted in cooperation with the U.S. Department of Transportation, Federal Highway Administration |
| 16.Abstract The overall objective of this research project was to evaluate the structural behavior of prestressed high-performance concrete (HPC) long-span bulb-tee girders utilized in Louisiana bridge construction. To accomplish this objective, one span of the Rigolets Pass Bridge was instrumented and monitored to obtain measured strain and deflection data for a period of one year after completion of construction. Four 131-ft long, BT-78 girders fabricated using HPC were instrumented to measure concrete strains and deflections at midspan. During fabrication of the four instrumented girders, representative samples of the prestressing strand and HPC were obtained and used for material property studies. After fabrication, the four instrumented girders were used to construct Span 43 of the Rigolets Pass Bridge. After erecting the instrumented girders at the bridge site, an HPC deck slab was added. During the deck slab construction for Span 43, instrumentation was added to measure concrete strains at midspan. Samples of the deck slab concrete were also obtained and used for material property studies. Throughout the bridge construction process, instrumentation readings were taken and recorded at selected time- or event-based intervals. After completion of the Rigolets Pass Bridge construction, the strain gauge instrumentation installed in the HPC girders and deck slab of Span 43 were connected to an automated on-site data acquisition system with remote access capabilities. The on-site data acquisition system was used to record concrete temperature and strain data at selected time increments for a period of one year after completion of construction. Manual measurements of midspan deflections were taken for Span 43 at the beginning, middle and end of the one-year bridge monitoring period. This Final Report documents results from both instrumentation monitoring and material property studies performed for Span 43 of the Rigolets Pass Bridge. The results obtained from this research provide detailed information related to the long-term behavior of a long-span structure fabricated using HPC. Findings and conclusions drawn from this research can be used by the Louisiana Department of Transportation and Development to develop specifications and designs for future HPC bridge structures. |
| 17.Key Words | 18.Distribution Statement Unrestricted. This document is available through the National Technical Information Service, Springfield, Va 21161 |
| 19.Security Classif.(of this report) | 20.Security Classif.(of this page) | 21.No. of Pages 74 | 22.Price |

Project Review Committee

Each research project will have an advisory committee appointed by the LTRC Director. The Project Review Committee is responsible for assisting the LTRC Administrator or Manager in the development of acceptable research problem statements, requests for proposals, review of research proposals, oversight of approved research projects, and implementation of findings.

LTRC appreciates the dedication of the following Project Review Committee Members in guiding this research study to fruition.

LTRC Administrator / Manager

Walid R. Alaywan

Members

Paul Fossier			LADOTD Bridge Design

Gill Gautreau		LADOTD Bridge Maintenance

Mike Ricca			LADOTD Construction

John Eggers			LADOTD Construction

Masood Rasoulian		LADOTD Contract Services

Michael B. Boudreaux	LTRC Implementation Engineer

Arturo Aguirre		FHWA

Directorate Implementation Sponsor

William B. Temple

STRUCTURAL MONITORING OF RIGOLETS PASS BRIDGE

FINAL REPORT

by

Robert N. Bruce, Jr.

Catherine and Henry Boh Chair Emeritus in Civil Engineering, Tulane University

New Orleans, LA  70118

John J. Roller

Principal Structural Engineer, CTLGroup

Skokie, IL  60077

Henry G. Russell

Engineering Consultant, Henry G. Russell, Inc.

Glenview, IL  60025

LTRC Project No. 04-2ST

State Project No. 736-99-1215

conducted for

Louisiana Department of Transportation and Development

Louisiana Transportation Research Center

The contents of this report reflect the views of the authors who are responsible for the facts and the accuracy of the data presented herein.  The contents do not necessarily reflect the official views or policies of the Louisiana Transportation Research Center, or the Louisiana Department of Transportation and Development.  This report does not constitute a standard, specification, or regulation.

December 2008

# ABSTRACT

The overall objective of this research project was to evaluate the structural behavior of prestressed high-performance concrete (HPC) long-span bulb-tee girders utilized in Louisiana bridge construction.  To accomplish this objective, one span of the Rigolets Pass Bridge was instrumented and monitored to obtain measured strain and deflection data for a period of one year after construction.  Four 131-ft long, BT-78 girders fabricated using HPC were instrumented to measure concrete strains and deflections at midspan.  During fabrication of the four instrumented girders, representative samples of the prestressing strand and HPC were obtained and used for material property studies.  After fabrication, the four instrumented girders were used to construct Span 43 of the Rigolets Pass Bridge.

After erecting the instrumented girders at the bridge site, an HPC deck slab was added.  During the deck slab construction for Span 43, instrumentation was added to measure concrete strains at midspan.  Samples of the deck slab concrete were also obtained and used for material property studies.

Throughout the bridge construction process, instrumentation readings were taken and recorded at selected time- or event-based intervals.  After completion of the Rigolets Pass Bridge construction, the strain gauge instrumentation installed in the HPC girders and deck slab of Span 43 were connected to an automated on-site data acquisition system with remote access capabilities.  The on-site data acquisition system was used to record concrete temperature and strain data at selected time increments for a period of one year after construction.  Manual measurements of midspan deflections were taken for Span 43 at the beginning, middle, and end of the one-year bridge monitoring period.

This final report documents results from both instrumentation monitoring and material property studies performed for Span 43 of the Rigolets Pass Bridge.  The results obtained from this research provide detailed information related to the long-term behavior of a long-span structure fabricated using HPC.  Findings and conclusions drawn from this research can be used by the Louisiana Department of Transportation and Development to develop specifications and designs for future HPC bridge structures.

# ACKNOWLEDGEMENTS

Work on this project was performed jointly by Tulane University Department of Civil and Environmental Engineering, CTLGroup, and Henry G. Russell, Inc. under the sponsorship of the Louisiana Transportation Research Center and in cooperation with the Louisiana Department of Transportation and Development.  Overall design and development of project specifications for the Rigolets Pass Bridge was performed by the Louisiana Department of Transportation and Development.  Paul B. Fossier, bridge engineer administrator of the Louisiana Department of Transportation and Development, provided technical guidance throughout the project.  Walid Alaywan, senior structures research engineer of the Louisiana Transportation Research Center, provided administrative management for the project.  John Eggers, Sadi Torres, and Randy Young were responsible for the concrete materials test program, and they provided valuable assistance with instrumentation readings at the precast yard and bridge site.

Appreciation is expressed to the staff of Gulf Coast Pre-Stress, Inc. of Pass Christian, MS, especially Don Theobald, for their patience during fabrication, storage, and shipping of the four instrumented girders.

Appreciation is also expressed to the staff of Massman Construction Company of Kansas City, MO, especially Steve Hayes and Terrence Colombatto, for their patience and assistance provided during construction of the instrumented span at the Rigolets Pass Bridge site.

IMPLEMENTATION STATEMENT

The Rigolets Pass Bridge is a 62-span bridge with a total length of 5489 ft. (1673 m) located on Routes US 90 and LA 433 in Orleans and St Tammany Parishes, LA.  Span lengths range from 19.7 ft. (6 m) to 254 ft. (77.5 m).  HPC was incorporated in two of the 62 bridge spans (Spans 42 and 43).  Spans 42 and 43 of the bridge comprise a continuous unit with span lengths of 131 ft. (40 m).  The spans utilize four lines of 78-in. (1.98-m) deep precast, prestressed concrete BT-78 girders spaced at 12-ft. 7-in. (3.83-m) centers.  Specified concrete compressive strength for the girders is 10,000 psi (69 MPa) at 56 days and 6670 psi (46 MPa) at release.

In conjunction with the construction of the Rigolets Pass Bridge, the state initiated a research program with the objective of monitoring the structural behavior of one of the two HPC bridge spans.  HPC Span 43 was instrumented to measure concrete strains and deflections at midspan for a period of one year after construction.  Material property studies were also included in the research effort.  Results from this material testing and structural monitoring program provide additional information for Louisiana’s growing HPC database and provide performance data related to an implementation project involving a relatively long span length.  This data will be useful in the development of specifications and designs for future HPC bridge structures.

TABLE OF CONTENTS

ABSTRACT	iii

ACKNOWLEDGEMENTS	v

IMPLEMENTATION STATEMENT	vii

TABLE OF CONTENTS	ix

LIST OF TABLES	xi

LIST OF FIGURES	xiii

INTRODUCTION	1

OBJECTIVES	3

SCOPE	5

METHODOLOGY	7

Bridge Description	7

Fabrication of HPC Girders	8

Instrumentation of HPC Bridge Span	13

Prestressing Forces	13

Concrete Strains	14

Girder Deflections	16

On-Site Automated Data Acquisition System	17

Material Property Testing Program	18

Prestressing Strand	18

Girder Concrete	18

Deck Slab Concrete	18

DISCUSSION OF RESULTS	21

Girder Concrete Material Properties	21

Prestressing Strand Material Properties	28

Deck Slab Concrete Material Properties	29

Prestressing Forces	30

Prestress Losses	31

Girder Deflections	39

Deck Strains	43

Seasonal Temperature and Strain Fluctuations	44

Winter Temperature and Strain Data	45

Summer Temperature and Strain Data	47

CONCLUSIONS	51

RECOMMENDATIONS	55

ACRONYMS, ABBREVIATIONS, AND SYMBOLS	57

REFERENCES	59

LIST OF TABLES

Table 1	Mix proportions for HPC girders	11

Table 2	HPC compressive strength results measured by GCP	13

Table 3	Girder concrete testing program	19

Table 4	Deck slab concrete testing program	20

Table 5	Girder concrete material properties	22

Table 6	Prestressing strand material properties	28

Table 7	Deck slab concrete material properties	29

Table 8	Measured average strand forces	31

Table 9	Prestress loss calculation scenarios	34

Table 10	Measured and calculated prestress losses using AASHTO Standard Specifications	35

Table 11	Measured and calculated prestress losses using AASHTO LRFD Bridge Design Specifications	38

Table 12	Measured and calculated girder deflections	41

# LIST OF FIGURES

Figure 1	Rigolets Pass Bridge	7

Figure 2	Cross section thru HPC bridge span	9

Figure 3	Initial curing temperatures measured by GCP at midspan	12

Figure 4	Load cells installed on selected prestressing strands	14

Figure 5	Vibrating wire strain gage instrumentation	15

Figure 6	Typical elevation reference point	16

Figure 7	Average concrete compressive strength versus age	21

Figure 8	Concrete modulus of elasticity versus compressive strength	23

Figure 9	Concrete modulus of rupture versus compressive strength	24

Figure 10	Creep coefficient versus concrete age	26

Figure 11	Concrete shrinkage versus age	27

Figure 12	Measured concrete strain versus time for Girders 43A, 43B, 43C, and 43D	32

Figure 13	Average prestress loss versus time	34

Figure 14	Measured midspan deflection versus time	40

Figure 15	Deck slab concrete strain versus time	44

Figure 16	Measured concrete temperature data – February 2008	45

Figure 17	Measured concrete strain data – February 2008	46

Figure 18	Measured concrete temperature data – August 2008	48

Figure 19	Measured concrete strain data – August 2008	49

# INTRODUCTION

The Louisiana Department of Transportation and Development (LADOTD) have been gradually introducing high performance concrete into their bridge construction programs.  At the same time, the Louisiana Transportation Research Center (LTRC) has been sponsoring research work to address design and construction issues related to utilization of high performance concrete.

In 1988, a bridge project was used as an experiment to determine if concrete with 8,000 psi (55 MPa) compressive strength could be obtained on a production product.  The experiment was only partially successful because the contractor was penalized on 68 percent of the project’s 2,370 ft. (723 m) of prestressed concrete girders.  In 1992, a 130-ft. (39.6-m) long, square prestressed concrete pile with a compressive strength of 10,453 psi (72.1 MPa) was successfully fabricated, shipped, and driven without damage as part of the State Route 415 bridge over the Missouri Pacific Railroad.  In 1993, two bridges on the Inner Loop Expressway near Shreveport were built using American Association of State Highway Transportation Officials (AASHTO) Type IV girders with a specified compressive strength of 8,500 psi (59 MPa) at an age of 28 days.

A 1994 LTRC report recommended that LADOTD consider the implementation of concrete with compressive strengths up to 10,000 psi (69 MPa) in a bridge and that the bridge should be instrumented to measure long-term behavior [1].  This recommendation was implemented with the design and construction of the Charenton Canal Bridge, which was opened to traffic in November 1999.  The successful construction of the Charenton Canal Bridge demonstrated that a high performance concrete bridge could be designed and built in Louisiana using locally available materials.

The Charenton Canal Bridge is a 365 ft. (111.3 m) long structure made up of five 73 ft. (22.3 m) spans, each incorporating five AASHTO Type III girders at 10 ft. (3.1 m) spacing.  In conjunction with the Charenton Canal Bridge Project, a parallel research and development project was undertaken that included provisions for instrumentation, monitoring of the completed bridge, and performing extensive concrete material property studies.  Based on the findings from this research, it was recommended that the LADOTD proceed with the implementation of HPC on all bridges where its use is deemed beneficial and economical [2].

After completion of the Charenton Canal Bridge research, the LADOTD was considering the use of deeper, longer-spanning HPC girders incorporating 0.6-in. (15.2 mm) diameter prestressing strands on future bridge projects.  To obtain test data that would provide assurance that these girders would perform satisfactorily, a research program was conducted to evaluate the structural performance of 72-in. (1.83 m) deep bulb-tee (BT) girders made with HPC under flexural fatigue, static shear, and static flexural loading conditions [3],[4].  Positive findings from this research paved the way for construction of the state’s second bridge incorporating HPC, the Rigolets Pass Bridge.

The Rigolets Pass Bridge is a 62-span bridge with a total length of 5,489 ft. (1673 m).  HPC was incorporated in two of the 62 bridge spans (Spans 42 and 43).  These spans each utilized four 131 ft. (40 m) long BT-78 girders at 12-ft. 7-in. (3.83-m) spacing.  In conjunction with the Rigolets Pass Bridge Project, the state initiated a research program with the objective of monitoring the structural behavior of one of the two HPC bridge spans.  HPC Span 43 was instrumented to measure concrete strains and deflections at midspan for a period of one year after of construction.  Material property studies were also included in the research effort.

# OBJECTIVES

The overall objective of the research described in the report was to monitor the behavior of a single HPC span incorporated in the Rigolets Pass Bridge for the purpose of obtaining data that will be useful in the development of specifications and designs for future HPC bridge structures.

Specific objectives of the research were as follows:

- Obtain and measure strain and deflection data from one instrumented span of the Rigolets Pass Bridge.

- Obtain material property data for the prestressing strand and concrete used in the superstructure of the instrumented span.

Evaluate the measured data based on recognized analytical or design methodologies.

SCOPE

The objectives of the research were achieved with the following scope of activities:

- Develop instrumentation, material property testing, and data collection plan.

- Attend meetings with precast fabricator and bridge construction contractor to address research project requirements.

- Instrument four 131-ft. (39.9-m) long, BT-78 girders fabricated for Span 43 of the Rigolets Pass Bridge.

- Install additional strain measurement instrumentation in the deck slab for Span 43 of the Rigolets Pass Bridge.

- Conduct material property tests on representative samples of the concrete and prestressing strand incorporated in the four instrumented girders.

- Conduct material property tests on representative samples of the concrete incorporated in the deck slab of Span 43.

- Measure and document concrete strains and midspan deflections at selected time- or event-based intervals.

- Install and setup on-site automated data acquisition system with remote access capabilities.

- Monitor the behavior of Span 43 of the Rigolets Pass Bridge for a period of one year after completion using both the data collected from the automated data acquisition system and data from limited manual deflection measurements taken at the bridge site.

- Conduct analysis of data.

Prepare the final report.

# METHODOLOGY

Bridge Description

The Rigolets Pass Bridge, shown in figure 1, is a 62-span bridge with a total length of 5,489 ft. (1673 m) located on Routes US 90 and LA 433 in Orleans and St Tammany Parishes, Louisiana.  Eighteen of the 62 bridge spans are 19.7-ft. (6-m) long slab spans used adjacent to the approach slab at each end of the bridge.  The slab spans transition into a series of five or six 49.2-ft. (15-m) long spans supported by AASHTO Type II girders near each end of the bridge.  The Type II girders near each end of the bridge transition into a series of fifteen 131.2-ft. (40-m) long spans that are supported by BT-78 girders.  These thirty BT-78 spans make up approximately 70 percent of the total bridge length.  The BT-78 girders transition into a 656.2-ft. (200-m) long center section comprised of a 3-span continuous girder.

Figure 1
Rigolets Pass Bridge

Structural design of the Rigolets Pass Bridge was in accordance with AASHTO Standard Specifications for Highway Bridges, Sixteenth Edition, (as amended by the current AASHTO Interim Specifications) [5].  The design live load for the bridge was based on the MS-18 (truck or lane) or HST-18(M) condition, whichever governed.  In addition to self weight, the bridge was also designed for a future wearing surface dead load equal to 12.5 lb./ft2.(600 N/m2.

Construction of the Rigolets Pass Bridge was in accordance with the Louisiana Standard Specifications for Roads and Bridges, 2006 Edition [6].  The precast concrete used for most of the superstructure girders was specified to be Class “P(X).”  However, two of the 62 bridge spans (Spans 42 and 43) were constructed using girders made with HPC.  The HPC used in the girders of Spans 42 and 43 was specified to be Class “P(HPC).”  The cast-in-place concretes used in the superstructure and substructure were specified to be Class “AA” and Class “A,” respectively.

Each of the girder-supported bridge spans incorporated an 8-in. (203-mm) thick cast-in-place reinforced concrete deck slab with a specified 28-day concrete compressive strength of 4,200 psi (29 MPa).  The bridge deck was designed as continuous over multiple span lengths with the main reinforcement oriented perpendicular to the direction of traffic.  The main deck slab reinforcement oriented perpendicular to the traffic consisted of two layers (top and bottom) of No. 6 (19 mm) deformed, Grade 60 bars spaced 6 in. (152 mm) apart.  Longitudinal reinforcement incorporated in the deck slab varied over the length and width of the span.

Fabrication of HPC Girders

HPC Spans 42 and 43 of the Rigolets Pass Bridge comprise a continuous unit with span lengths of 131 ft. (40 m).  These spans utilize four lines of 78-in. (1.98-m) deep precast, prestressed concrete BT-78 girders spaced at 12-ft. 7-in. (3.83-m) centers, supporting an 8-in. (200-mm) thick reinforced concrete deck as shown in figure 2.  The four HPC girders used in each span were assigned specific alphanumeric designations (42A, 42B, 42C, and 42D) according to their position.  The total width of the bridge deck is 45 ft. 11 in. (14 m).

All eight HPC BT-78 girders for the Rigolets Pass Bridge were fabricated by Gulf Coast Pre-Stress (GCP) located in Pass Christian, Mississippi.  The HPC girders each incorporate fifty-six 0.6-in. (15.2-mm) diameter strands in the lower flange.  Twelve of the 56 strands are debonded for various lengths at each end of the girders.  Each girder also incorporates four 3/8-in. (9.5-mm) diameter strands in the upper flange.  All strands used in the HPC girders

Figure 2
Cross section thru HPC bridge span

were specified to be low-relaxation material conforming to ASTM Designation: A416, Grade 270 (1860 MPa).

During fabrication, all strands were stressed over a bed length of 527 ft. 1-1/4 in. (160,661 mm).  The specified initial tension force for the 3/8-in. (9.5-mm) diameter strands in the upper flange was 10 kips (44.5 kN) or approximately 50 percent of the minimum strand breaking strength.  The specified initial tension force for the 0.6-in. (15.2-mm) diameter strands in the lower flange was 43.95 kips (195.5 kN).  This initial tension force corresponds with 75 percent of the specified minimum strand breaking strength.

GCP utilized a calibrated hydraulic jack to apply initial tension to the prestressing strands.   Tensioning was executed by first applying a 2-kip (8.9 kN) pre-load to the strand.  After applying the pre-load, tensioning continued by pulling the strand to the specified 43.95 kip (195.5 kN) initial force.  The force applied to each strand was confirmed by comparing measured elongation values with a corresponding calculated value determined based on the specified force, the overall bed length between anchorage points, and an assumed strand modulus of elasticity equal to 28,800 ksi (198.6 GPa).  The elongation calculation also included allowance for seating losses at each end.  During the stressing of each strand, the force reading taken from the stressing unit and corresponding measured elongation value were documented by GCP on their daily production report.

After stressing all of the strands, shear and anchorage zone reinforcement were installed and secured at the required locations.  Mats of mild reinforcement were also installed along the top flange of each girder.  All mild reinforcement incorporated in the HPC girders was specified to conform to ASTM Designation: A615, Grade 60 (420 MPa).  Once all the mild reinforcement had been secured, lifting loops were installed near each end, and the steel side forms were oiled and moved into place.  After securing the side forms, the bed was ready for the concrete pour.

The eight girders required for the two HPC spans (Spans 42 and 43) were fabricated using three separate castings or pours.  Girders 42A, 43A, and 43B were poured on October 31, 2006.  Girders 42B, 43C, and 43D were poured on November 8, 2006.  Girders 42C and 42D were poured on November 14, 2006.  Specified concrete compressive strength for the HPC girders is 10,000 psi (69 MPa) at 56 days and 6,670 psi (46 MPa) at release.  The concrete mix proportions used by GCP for fabrication of the HPC girders is shown in table 1.  The fresh concrete was transported from the batch plant and placed in the forms using standard Tuckerbuilt(  concrete transport vehicles.  Prior to placement, the measured slump of the concrete produced for all three pours ranged from 6-1/2 to 9 in (165 to 229 mm).  Once placed in the forms, the concrete was consolidated using both external and interval vibrators.  Each of the HPC girders required approximately 37.2 cu yds (28.5 m3) of concrete.

Table 1
Mix proportions for HPC girders

| Material | Quantities |
| --- | --- |
|  | per yd3 | per m3 |
| Portland Cement Type III | 846 lb. | 384 kg |
| Silica Fume | 100 lb. | 45 kg |
| Fine Aggregate | 1,149 lb. | 521 kg |
| Course Aggregate - Limestone | 1,866 lb. | 846 kg |
| Water | 204 lb. | 93 kg |
| Water Reducer, ASTM C494 - Type D | 38 oz | 1,124 ml |
| High-Range Water Reducer, ASTM C494 – Type F | 51 oz | 1,508 ml |
| Air Entrainment | None | None |
| Water/Cementitious Materials Ratio | 0.22 | 0.22 |

Immediately after placing the concrete, the bed was covered with a tarpaulin that remained in place until the required release strength was achieved.  None of the HPC girders for the Rigolets Pass Bridge required steam curing.  During the initial curing period, GCP monitored concrete temperatures at the middle and both ends of the casting bed.  Concrete temperatures measured during the initial curing period in the bottom flange of a girder near midspan for two of the three HPC pours are shown in figure 3.   Based on the data in figure 3, the concrete in the bottom flange near midspan achieved a maximum temperature of approximately 153 ºF (67 ºC) for both pours.  The maximum temperature was achieved approximately 12 hours after completion of the pour and then started to decrease at a rate of approximately 3 ºF (1.5 ºC) per hour.

GCP produced several match-cured cylinders during the three HPC girder pours.  These cylinders were made in 4 x 8-in. (102 x 203-mm) molds and were cured to match the temperature measured in the girder lower flange region.  The match curing regime began immediately after the pour ended and continued until a cylinder break indicated that the required release strength had been achieved.  After initial curing, the cylinders were stripped and cured under ambient conditions in the plant until tested.  Results from all compressive strength tests performed by GCP on match-cured cylinders they produced for the three HPC pours are shown in table 2.  As indicated by the data in table 2, the required release strength of 6,670 psi (46 MPa) was typically achieved within 15 hours after completion of the pour.

Figure 3
Initial curing temperatures measured by GCP at midspan

After achieving the required release strength, the tarpaulin used to cover the bed and the steel side forms were removed.  Release of the prestressing strands then commenced, following the detensioning sequence shown on the GCP girder fabrication drawings.  After release of the strands, the girders were moved into storage until needed at the bridge site.

Table 2
HPC compressive strength results measured by GCP

| Concrete Age | Concrete compressive strength |
| --- | --- |
|  | Pour 42A, 43A, 43B | Pour 42B, 43C, 43D | Pour 42C, 42D |
|  | psi | MPa | psi | MPa | psi | MPa |
| Release | 7,570a | 52 | 8,840b | 61 | 9,180a | 63 |
|  | — | — | 9,010b | 62 | 8,610a | 59 |
| 14 days | 9,000 | 62 | — | — | — | — |
|  | 10,620 | 73 | — | — | — | — |
| 28 days | 10,840 | 75 | 10,770 | 74 | 10,130 | 70 |
|  | 10,630 | 73 | 10,850 | 75 | 10,140 | 70 |
|  | 10,390 | 72 | 11,200 | 77 | 10,660 | 74 |

a	Release strength measured at an age of 15 hours.

b	Release strength measured at an age of 17.5 hours.

—	Test not performed at designated age.

Instrumentation of HPC Bridge Span

In conjunction with the construction of the Rigolets Pass Bridge, the state initiated a research program with the objective of monitoring the structural behavior of one of the two HPC bridge spans.  The four HPC BT-78 girders and the deck slab for Span 43 of the Rigolets Pass Bridge were instrumented to monitor prestressing forces, concrete strains, and deflections.  Details associated with each type of instrumentation were as follows.

Prestressing Forces

During fabrication of the BT-78 girders for Span 43, six of the 54 prestressing strands were instrumented with load cells to measure strand force levels beginning at the time of initial tensioning and continuing until release.  Prior to stressing, load cells were installed on selected strands at the dead end (anchorage end) of the bed.  The specific strands that were instrumented with load cells are indicated in figure 4.  Individual load cell readings were made before stressing (zero reading), after stressing the instrumented strand, after stressing all strands, prior to concrete placement, after concrete placement, prior to strand release, and after strand release (return to zero load).  Additional interim load cell readings were taken at selected time-based intervals.

Figure 4
Load cells installed on selected prestressing strands

Concrete Strains

Five vibrating wire strain gages (VWSGs) were installed at midspan of each of the four instrumented girders to monitor concrete strains and prestress losses.  Each VWSG incorporated a thermistor for measuring the concrete temperature associated with each strain measurement.  As indicated in figure 5, three of the VWSGs were installed in the lower flange at the elevation of the strand group centroid.  The remaining two gages were installed at the center of gravity of the top flange located approximately 3 in. (76 mm) down from the top surface of the girder.  During construction, readings for the VWSGs installed in each girder were taken after installation, prior to concrete placement, after concrete placement, prior to strand release, after strand release, after girder storage, at a concrete age of 28 days, once a month for the next two months, before shipping, after erection, and before and after casting the deck slab concrete.

Figure 5
Vibrating wire strain gage instrumentation

Seven additional VWSGs were installed in the deck slab of Span 43 at midspan.  As indicated in figure 5, the VWSGs in the deck slab were installed directly above each girder and at the mid-point between each of the four girders.  All seven of these VWSGs were installed at mid-depth in the 8-in. (203-mm) thick deck slab.  During construction, readings for the VWSGs installed in the deck slab were taken after installation and before and after casting the deck slab concrete.

After casting the deck slab concrete, readings for all the VWSGs installed in both the girders and deck slab were taken once a week for the first month and once a month until the on-site data acquisition system (DAS) was installed.

Girder Deflections

Three elevation reference points were embedded along the top flange of each of the four instrumented girders.  These points were embedded at midspan and near both ends to provide a permanent reference for girder deflection measurements.  Each reference point consisted of a threaded steel stud with a machined indentation at one end.  Each point was embedded with the indentation end protruding from the concrete surface approximately 1 in.  Acorn capping nuts were threaded on the protruding end of each stud to protect the machined indentation from weather.  A photograph of a typical reference point is shown in fig. 6.

Figure 6
Typical elevation reference point

Girder deflection measurements required the use of a standard surveyor’s level and tripod.  However, the custom steel rod used for the measurements incorporated a machined conical point at one end to interface with the indentation on the top of each elevation reference point, a stainless steel ruler with smallest measurement divisions of 1/16 in. (1.6 mm), and a reference plumb bubble.  Deflection measurements were made using the level to sight elevations at each reference point location.  Based on these measurements, the deflection was calculated by subtracting the average elevation of the two girder ends from the midspan elevation.

During construction, girder midspan deflection measurements were made prior to strand release, after strand release, after girder storage, at a concrete age of 28 days, once a month for the next two months, before shipping, after erection, and before and after deck casting.  Prior to casting the deck slab, the elevation reference points embedded in the top surface of each girder were extended to the elevation of the finished surface of the deck slab.  After casting the deck slab, deflection measurements were made once a week for the first month, once a month for the first three months, and every 6 months during the one-year monitoring period.

On-Site Automated Data Acquisition System

During construction of Span 43, the lead wires for the twenty-seven embedded VWSGs were routed to the south side where they exited the side of the deck slab at a common location near midspan.  From the point of exit, the lead wires were routed in a single conduit to a large enclosure box mounted on the south barrier railing.  Provisions for providing 120V electrical power and telephone service at the enclosure box were made by the bridge construction contractor.  After construction of the instrumented bridge span had been completed, an on-site DAS with remote access and data collection capabilities was installed within the enclosure.  After installation, the VWSGs were connected to the DAS, communications were established, and the system was programmed to collect data at established time increments.

After completion of the Rigolets Pass Bridge, data from VWSGs installed in the girders and deck slab was recorded over a one -year monitoring period.  During this period, data from all VWSGs were read and stored once per hour.  Stored data was downloaded via remote telephone modem access once a week and checked against previously stored data to ensure that the system is functioning properly.

### Material Property Testing Program

Prestressing Strand

During fabrication of the four instrumented girders, representative samples of 0.6-in. (15.2-mm) diameter prestressing strands were taken for material property tests.  One 5-ft. (1.52-m) long sample was taken from each of the seven coils of strands used.  The strand samples were tested to determine breaking strength, 1 percent elongation load (yield), modulus of elasticity, and total elongation.

Girder Concrete

Material property tests were performed on specimens representing concrete placed in the midspan region of each of the four instrumented girders.  Concrete compressive strength (ASTM C 39), modulus of elasticity, (ASTM C 469), unit weight, modulus of rupture (ASTM C 78), coefficient of thermal expansion (CRD C-39), creep and shrinkage (ASTM C 512), and permeability (ASTM C 1202) tests were performed according to the schedule shown in table 3.  Concrete cylinders used for compressive strength and modulus of elasticity tests were “match-cured” to match the temperature in the lower flange of each corresponding girder.  Other “field-cured” specimens were covered with plastic and stored on tables situated adjacent to the casting bed.  Just prior to release of the strands, all of the match- and field-cured specimens were stripped from the molds.  The field-cured specimens required for coefficient of thermal expansion, creep, and shrinkage tests scheduled to commence at an age of three days were shipped to CTLGroup.  All other specimens were transported to LTRC for storage and future testing.

Deck Slab Concrete

Material property tests were performed on specimens representing the concrete placed in the midspan region of Span 43.  Concrete compressive strength (ASTM C 39), modulus of elasticity (ASTM C 469), unit weight, modulus of rupture (ASTM C78), coefficient of thermal expansion (CRD C-39), and permeability (ASTM C1202) tests were performed in accordance to the schedule shown in table 4.  All of the specimens required for the deck slab concrete test program were initially field-cured at the bridge site.  The specimens required for coefficient of thermal expansion tests scheduled to commence at an age of three days were shipped to CTLGroup the day after the deck slab was poured.  All other specimens were transported to LTRC for storage and future testing.

Table 3
Girder concrete testing program

| Girder | Compressive strength and modulus of elasticity test specimens (4x8-in cylinder) | Modulus of rupture test specimens (6 x 6 x 20-in. beam) | Permeability test specimens (6 x 12-in. cylinder) | Coefficient of thermal expansion test specimens (6 x12-in. cylinder) | Creep and shrinkage test specimens (6 x 12-in. cylinder) |
| --- | --- | --- | --- | --- | --- |
|  | Initial curing method | Test age, days | Initial curing method | Test age, days | Initial curing method | Test age, days | Initial curing method | Test age, days | Initial curing method | Test age, days |
|  |  | R | 28 | 56 | 90 |  | 56 |  | 56 |  | 3 | 90 |  | 3 | 90 |
| 43A | Match | 3 | 3 | 3 | 3 | Field | 3 | Field | 3 | Field | — | — | Field | — | — |
| 43B | Match | 3 | 3 | 3 | 3 | Field | 3 | Field | 3 | Field | — | — | Field | — | — |
| 43C | Match | 3 | 3 | 3 | 3 | Field | 3 | Field | 3 | Field | — | — | Field | — | — |
| 43D | Match | 3 | 3 | 3 | 3 | Field | 3 | Field | 3 | Field | 3 | 3 | Field | 3 | 3 |

—	Test not performed at designated age.

Table 4
Deck slab concrete testing program

| Material property | Specimens assigned for each test age |
| --- | --- |
|  | 3 days | 7 days | 28 days | 56 days | 90 days |
| Compressive strength and modulus of elasticity test specimens (4 x 8-in cylinder) | — | 3 | 3 | — | 3 |
| Modulus of rupture test specimens (6 x 6 x 20-in. beam) | — | — | 3 | 3 | — |
| Permeability test specimens (6 x 12-in. cylinder) | — | — | — | 3 | — |
| Coefficient of thermal expansion test specimens (6 x 12-in. cylinder) | 3 | — | — | — | 3 |

— 	Test not performed at designated age.

DISCUSSION OF RESULTS

Girder Concrete Material Properties

Measurements of compressive strength, modulus of elasticity, modulus of rupture, chloride permeability, coefficient of thermal expansion, creep, and shrinkage were made on test specimens representing concrete placed in the midspan region of the instrumented girders.  Measured concrete properties, except creep and shrinkage, are presented in table 5.

Concrete compressive strength tests were performed in accordance with ASTM C 39 at four different test ages.  Average measured concrete compressive strength values for the four instrumented girders determined from tests of match-cured cylinders are shown in figure 7.  Based on previous research, it was determined that match-cured cylinders yielded higher measured concrete compressive strengths at all ages than field-cured cylinders [2].  Therefore, for this research, only match-cured cylinders were used to determine girder concrete compressive strength and modulus of elasticity properties. As indicated by the data presented in figure 7, the concrete used in the four instrumented girders exhibited very similar compressive strength values at all test ages.

Figure 7
Average concrete compressive strength versus age

Table 5
Girder concrete material properties

| Material Property | Specimen Size | Initial Curing | Girder | Concrete Age |
| --- | --- | --- | --- | --- |
|  |  |  |  | Release | 28 days | 56 days | 90 days |
| Compressive Strength,a psi | 4 x 8-in. cyl. | Match | 43A | 9,490 | 10,770 | 11,240 | 11,660 |
|  |  |  | 43B | 9,510 | 10,860 | 11,010 | 11,540 |
|  |  |  | 43C | 9,290 | 10,950 | 11,300 | 11,650 |
|  |  |  | 43D | 8,720 | 10,830 | 11,500 | 11,820 |
|  |  |  | Average | 9,253 | 10,853 | 11,263 | 11,668 |
| Modulus of Elasticity,a ksi | 4 x 8-in. cyl. | Match | 43A | 6,300 | 6,250 | 6,350 | 6,400 |
|  |  |  | 43B | 6,050 | 6,050 | 6,150 | 6,250 |
|  |  |  | 43C | 5,950 | 6,150 | 6,200 | 6,650 |
|  |  |  | 43D | 5,700 | 5,850 | 6,450 | 6,600 |
|  |  |  | Average | 6,000 | 6,075 | 6,288 | 6,475 |
| Unit Weight,a lb./ft3 | 4 x 8-in. cyl. | Match | 43A | 146.8 | 146.1 | 146.9 | 147.3 |
|  |  |  | 43B | 147.1 | 146.1 | 145.3 | 147.4 |
|  |  |  | 43C | 146.4 | 146.2 | 146.1 | 145.5 |
|  |  |  | 43D | 146.0 | 146.3 | 145.6 | 146.0 |
|  |  |  | Average | 146.6 | 146.2 | 146.0 | 146.6 |
| Modulus of Rupture,a psi | 6 x 6 x 20-in. beam | Field | 43A | — | — | 940 | — |
|  |  |  | 43B | — | — | 1,010 | — |
|  |  |  | 43C | — | — | 1,070 | — |
|  |  |  | 43D | — | — | 940 | — |
|  |  |  | Average | — | — | 990 | — |
| Permeability,a Coulombs | 6 x 12-in. cyl. | Field | 43A | — | — | 136 | — |
|  |  |  | 43B | — | — | 140 | — |
|  |  |  | 43C | — | — | 156 | — |
|  |  |  | 43D | — | — | 170 | — |
|  |  |  | Average | — | — | 151 | — |
| Coefficient of Thermal Expansion,b millionths/ºF | 6 x 12-in. cyl. | Field | 43D - 1 | — | 4.58 | — | 5.70 |
|  |  |  | 43D - 2 | — | 4.30 | — | 5.18 |
|  |  |  | 43D - 3 | — | 4.47 | — | 5.75 |
|  |  |  | Average | — | 4.45 | — | 5.54 |
|  |  |  | Overall Average = 5.00 |

a	Each reported test value represents the average for three individual tests.  Average values represent results from twelve individual tests.

b	Each reported test value represents one individual test.  Reported release values were measured at a concrete age of 28 days instead of the planned 3- day test.

—	Test not performed at designated age.

The specified concrete compressive strength for the HPC girders is 10,000 psi (69 MPa) at 56 days and 6,670 psi (46 MPa) at release.  As indicated by the data reported in table 5 and figure 7, the measured concrete compressive strengths for girders 43A, 43B, 43C, and 43D exceeded the specified strength at both the release and 56-day test ages.

Concrete modulus of elasticity tests were performed in accordance with ASTM C 469 at four different test ages.  Concrete modulus of elasticity versus compressive strength data for the four instrumented girders is presented in figure 8.   For the purpose of comparison, measured data obtained from other previous HPC research sponsored by LTRC is also shown in figure 8 [1], [2], [3].  The solid line shown in figure 8 represents the relationship between concrete compressive strength and modulus of elasticity given by the Ec = wc1.5 33 expression from Article 8.7.1 of the AASHTO Standard Specifications for Highway Bridges [5], where wc is taken as 145 pcf (2,323 kg/m3).  As indicated by the data presented in figure 8, the AASHTO Standard Specification relationship between compressive strength and modulus of elasticity appears to be reasonably consistent with the measured data for strength levels up to 10,000 psi (69 MPa).  However, correlation between the AASHTO expression and the measured data appears to diminish somewhat for higher compressive strength levels.

Figure 8
Concrete modulus of elasticity versus compressive strength

The data shown in figure 8 indicate that the AASTHO Standard Specification expression may tend to overestimate the modulus of elasticity for concrete with compressive strength exceeding 10,000 psi (69 MPa).  Consequently, it is recommended that the LADOTD consider using values that are slightly less than those predicted by the AASTHO expression whenever design concrete compressive strengths exceed 10,000 psi (69 MPa).  It is also recommended that the state continue to build upon their existing high-strength concrete modulus of elasticity database for the purpose of determining suitable reduction factors that could be applied to the AASHTO expression when needed.

Concrete modulus of rupture tests were performed in accordance with ASTM C 78 at an age of 56 days.  Concrete modulus of rupture versus compressive strength data for the four instrumented girders is presented in figure 9.   For the purpose of comparison, measured data obtained from other previous HPC research sponsored by LTRC is also shown in figure 9 [1], [2], [3].  The solid lines shown in figure 9 represent calculated relationships between concrete compressive strength and modulus of rupture using the expression fr = k , where the k factor is taken as either 7.5 (lower line) or 10 (upper line).  The fr = 7.5   line represents the relationship for modulus of rupture given in Article 9.15.2.3 of the AASHTO Standard Specifications for Highway Bridges [5].

Figure 9
Concrete modulus of rupture versus compressive strength

As indicated by the data presented in figure 9, the AASHTO Standard Specification relationship appears to consistently provide a conservative prediction of modulus of rupture for all strength levels investigated.  The variability of the measured modulus of rupture values is such that the use of k factors greater than the 7.5 value currently incorporated in the AASHTO Standard does not appear warranted.

Tests to determine the chloride permeability of the girder concrete were performed in accordance with ASTM C 1202 on field-cured 6 x 12-in. (152 x 305-mm) cylinders representing concrete place in the midspan of each instrumented girder.  The chloride permeability tests were performed at a concrete age of 56 days.  The average chloride permeability determined for the concrete used in the midspan region of Girders 43A, 43B, 43C, and 43D was 151 coulombs.  This average measured permeability value is considerably less than the 2,000 coulomb limit stipulated in the specifications for the Rigolets Pass Bridge project.

The average measured permeability value for the Rigolets Pass Bridge project is also considerably less than the average permeability value for the Charenton Canal Bridge project (1,355 coulombs) measured at a concrete age of 56 days [2].  The concrete mix design for the girders in the Charenton Canal Bridge incorporated 30 percent Class C fly ash by total weight of cementitious materials.  The HPC girders in the Rigolets Pass Bridge incorporated 11 percent silica fume by total weight of cementitious materials.  Therefore, it appears that the use of silica fume provides a much greater benefit relative to decreasing overall permeability than Class C fly ash.

Tests to determine the coefficient of thermal expansion for the girder concrete were performed in accordance with CRD-C39 on field-cured 6 x 12-in. (152 x 305-mm) cylinders representing concrete place in the midspan of Girder 43D.  It was originally planned that coefficient of thermal expansion tests would be performed at concrete ages of 3 and 90 days.  However, due to problems encountered during testing, the data for the 3-day test age was judged unreliable and was subsequently discarded and replaced with data from another test performed at an age of 28 days.  The average coefficient of thermal expansion for the girder concrete measured at test ages of 28 and 90 days were 4.45 millionths/ ºF (8.01 millionths/ ºC) and 5.54 millionths/ ºF (9.97 millionths/ ºC), respectively.  The overall average coefficient of thermal expansion for both test ages was 5.00 millionths/ ºF (9.00 millionths/ ºC.  This average measured value was subsequently used to correct measured concrete strains for temperature effects prior to use in prestress loss calculations.

Tests to determine creep and shrinkage properties for the girder concrete were performed in accordance with ASTM C 512 on field-cured 6 x 12-in (152 x 305-mm) cylinders representing concrete placed in the midspan region of Girder 43D.  It was originally planned that creep and shrinkage tests would be performed at concrete ages of 3 and 90 days.  However, due to delay in receiving the cylinders for the 90-day test age, the actual concrete age at the time the test commenced was 100 days.  Both the 3- and 100-day age creep and shrinkage tests were performed under ambient conditions of 73 ºF (23 ºC) and 50 percent relative humidity.  The planned test duration used for each age of loading was one year.  However, the duration of the 3-day age of loading test was extended to terminate at the same time as the 100-day age of loading test.  Measured creep coefficient, defined as the ratio of creep strain to initial strain, and shrinkage data for the two different ages of loading (3 and 100 days) are shown in figures 10 and 11, respectively.

Figure 10
Creep coefficient versus concrete age

Figure 11
Concrete shrinkage versus age

Prior to starting the creep tests, additional representative field-cured 6 x 12-in (152 x 305-mm) cylinders were tested in compression to determine compressive strength corresponding with each age of loading.  Three cylinders were tested for each age.  The measured concrete compressive strength for concrete ages of 3 and 90 days were 8,250 psi (57 MPa) and 12,210 psi (84 MPa), respectively.  These average compressive strength values were used as the basis for establishing the intensity of the load used for the creep tests.  For both test ages, the applied load used for creep testing corresponded to 40 percent of the measured concrete compressive strength at that age.

The measured creep coefficient and shrinkage data shown in figures 10 and 11 reflect two phenomena typically observed with conventional strength concretes; the rate of creep and shrinkage decreases with time, and the specific creep and total shrinkage is less for concrete tested at later ages. Recognizing that the four HPC girders fabricated for the instrumented bridge span first experience compressive stresses and significant drying conditions beginning at the time of form removal and strand release, the creep and shrinkage data for the 3-day age of loading condition would be expected to more closely represent the actual in-service response.

Based on the 3-day age of loading data, the creep coefficient after twelve months appears to be stabilizing at a value of approximately 2.50, and the shrinkage appears to be stabilizing at approximately 300 millionths.  According to the ACI Committee 209 Report (ACI 209R-92), the ultimate creep coefficient of concrete normally falls in the range of 1.30 to 4.15, and ultimate shrinkage will normally fall into the range of 415 to 1070 millionths [7].  The creep coefficient after one year reflected by the measure test data falls approximately in the middle of the expected range.  The measured shrinkage after one year falls well below the expected range. Based on these data, lower-than-normal measured girder prestress losses due to the combined effects of creep and shrinkage would be expected.

Prestressing Strand Material Properties

During fabrication of the four instrumented girders for Span 43, samples of 0.6-in. (15.2-mm) diameter prestressing strands were taken and tested to determine breaking strength, 1 percent elongation load (yield), modulus of elasticity, and total elongation.  Results from the strand tests are presented in table 6.  All applicable measured strand material properties reported in table 6 satisfied the corresponding specification requirements of ASTM Designation: A416.  As indicated in table 6, the average measured modulus of elasticity for the seven strand lots tested was 27,950 ksi (193 MPa).

Table 6
Prestressing strand material properties

| Strand Lot / Serial Number | 1 Percent Elongation Load, lbf | Breaking Load, lbf | Total Elongation Under Load, percent | Modulus of Elasticity, ksi |
| --- | --- | --- | --- | --- |
| 130146679326 | 55,200 | 59,600 | 6.1 | 28,300 |
| 130146679327 | 54,900 | 59,800 | 6.5 | 27,050 |
| 130146679328 | 55,200 | 59,400 | 5.0 | 27,850 |
| 130146679331 | 54,800 | 59,800 | 5.9 | 28,250 |
| 130146679332 | 56,000 | 60,000 | 5.1 | 28,650 |
| 130146679335 | 54,800 | 59,800 | 5.9 | 27,700 |
| 130146679342 | 54,800 | 59,600 | 6.0 | 27,950 |
| Average | 55,100 | 59,700 | 5.8 | 27,950 |

Deck Slab Concrete Material Properties

Measurement of compressive strength, modulus of elasticity, modulus of rupture, chloride permeability, and coefficient of thermal expansion were made on test specimens representing concrete placed in the midspan region of the deck slab for Span 43.  Measured concrete properties are presented in table 7.

Table 7
Deck slab concrete material properties

| Material Property | Specimen Size | Initial Curing | Cyl. | Concrete Age |
| --- | --- | --- | --- | --- |
|  |  |  |  | 3 days | 7 days | 28 days | 56 days | 90 days |
| Compressive Strength,a psi | 6 x 12-in. cyl. | Field | 1 | — | 5,850 | 7,880 | — | 8,570 |
|  |  |  | 2 | — | 5,580 | 7,790 | — | 8,870 |
|  |  |  | 3 | — | 5,600 | 7,600 | — | 8,670 |
|  |  |  | Ave | — | 5,677 | 7,757 | — | 8,703 |
| Modulus of Elasticity,a ksi | 6 x 12-in. cyl. | Field | 1 | — | 5,100 | 5,850 | — | 6,450 |
|  |  |  | 2 | — | 5,250 | 5,350 | — | 6,350 |
|  |  |  | 3 | — | 5,050 | 5,700 | — | 6,500 |
|  |  |  | Ave | — | 5,133 | 5,633 | — | 6,433 |
| Unit Weight,a lb./ft3 | 6 x 12-in. cyl. | Field | 1 | — | 143.7 | 145.1 | — | 145.1 |
|  |  |  | 2 | — | 144.3 | 144.2 | — | 143.9 |
|  |  |  | 3 | — | 144.6 | 144.7 | — | 144.7 |
|  |  |  | Ave | — | 144.2 | 144.7 | — | 144.6 |
| Modulus of Rupture,a psi | 6 x 6 x 20-in. beam | Field | 1 | — | — | 730 | 630 | — |
|  |  |  | 2 | — | — | 760 | 640 | — |
|  |  |  | 3 | — | — | 800 | 590 | — |
|  |  |  | Ave | — | — | 763 | 620 | — |
| Permeability,a Coulombs | 6 x 12-in. cyl. | Field | 1 | — | — | — | 1,115 | — |
|  |  |  | 2 | — | — | — | 1,146 | — |
|  |  |  | 3 | — | — | — | 824 | — |
|  |  |  | Ave | — | — | — | 1,028 | — |
| Coefficient of Thermal Expansion,a millionths/ºF | 6 x 12-in. cyl. | Field | 1 | 6.47 | — | — | — | 5.93 |
|  |  |  | 2 | 5.58 | — | — | — | 5.40 |
|  |  |  | 3 | 6.11 | — | — | — | 5.35 |
|  |  |  | Ave | 6.05 | — | — | — | 5.56 |
|  |  |  | Overall Average = 5.81 |

a	Each reported test value represents one  individual tests.  Average values represent results from three individual tests.

—	Test not performed at designated age.

The specified concrete compressive strength for the deck slab is 4,200 psi (29 MPa) at 28 days.  As indicated by the data reported in table 7, the measured concrete compressive strengths at all test ages exceeded the specified strength.

Tests to determine the chloride permeability of the deck slab concrete were performed in accordance with ASTM C 1202 on field-cured 6 x 12-in. (152 x 305-mm) cylinders representing concrete place at midspan.  The chloride permeability tests were performed at a concrete age of 56 days.  As indicated by the data reported in table 7, the average measured chloride permeability for the deck slab concrete was 1,028 coulombs.  This average measured permeability value is less than the 2,000 coulomb limit stipulated in the specifications for the Rigolets Pass Bridge project.

Prestressing Forces

Each girder was fabricated using uncoated, Grade 270 (1860 MPa), low-relaxation, seven-wire strand conforming to ASTM A416.  The specified initial tensile force for each 0.6-in. (15.2-mm) diameter strand was 43.95 kips (195.9 kN), which corresponds to 75 percent of the specified minimum strand breaking strength.  During fabrication of the four instrumented girders for Span 43, load cells were installed on six selected prestressing strands between the dead end anchorage and the bulkhead.  Strands selected for load cell instrumentation are shown in figure 4.  Using these load cells, the force levels in the selected strands were measured at various time- or event-based intervals, beginning at the time of initial tensioning and continuing until release.

The four instrumented girders were fabricated during two separate production runs.  The first production run included instrumented girders 43A and 43B.  The second production run included girders 43C and 43D.  Average measured strand force values for both production runs recorded after stressing all strands and just prior to release are shown in table 8.  Each value reported in table 8 represents the average reading for five of the six load cells.  During stressing, one of the six load cells tipped due to inadequate bearing support on the bulkhead surface.  Upon discovering this condition, the load cell was removed and the strand was re-stressed without load cell instrumentation.  This incident occurred for both production runs.

As indicated by the data in table 8, the average measured force levels after stressing all of the strands were 4.4 to 4.9 percent less than the specified 43.95 kip (195.5 kN) initial force.  However, these measured reduction values were still within the 5 percent tolerance cited in the PCI Manual for Quality Control [8].

Table 8
Measured average strand forces

| Girder Production Run | Average measured force after stressing all strands | Average measured force prior to release of prestress |
| --- | --- | --- |
|  | kips | kN | Percent reduction | kips | kN | Percent reduction |
| 43A and 43B | 42.01 | 186.9 | 4.4 | 40.94 | 182.1 | 6.8 |
| 43C and 43D | 41.80 | 186.0 | 4.9 | 40.04 | 178.1 | 8.9 |
| Average | 41.90 | 186.4 | 4.7 | 40.49 | 180.1 | 7.9 |
| Specified | 43.95 | 195.5 | < 5.0 | — | — | — |

Prior to releasing the prestress, the average force levels were 6.8 to 8.9 percent less than the specified initial force.  As indicated in figure 3, measured concrete temperatures at the time of release were still quite high.  Therefore, thermal expansion of the embedded strands likely contributed to the reduction in prestress force reported in table 8.  It should also be noted that the overall time duration between stressing and release for the production run incorporating Girders 43C and 43D (70.5 hours) was longer than the duration for the production run incorporating Girders 43A and 43B (48 hours).  This difference in overall production duration may have contributed to the noted difference in the measured force reduction between the two production runs.

Prestress Losses

Vibrating wire strain gages (VWSGs) were installed at midspan in each of the four instrumented HPC girders of Span 43, as shown in figure 5.  For each of these girders, the three VWSGs installed in the bottom flange at the center of gravity of the prestressing strands were used to determine prestress losses.  The two VWSGs installed in the top flange of each girder provided a second reference point for girder section strain measurements, which could be used as a means of validating the overall response to creep, shrinkage, and temperature deformations as well as external load effects.   Each VWSG included a thermistor for measuring concrete temperature associated with each strain measurement.  Plots of average measured concrete strain versus time for VWSGs installed in each girder are shown in figure 12.

Figure 12
Measured concrete strain versus time for Girders 43A, 43B, 43C and 43D

The plotted average values shown in figure 12 were based on individual strain readings that were adjusted to a constant temperature.  The temperature correction applied to the individual strain readings was calculated based on the measured concrete temperature associated with the reading, the average measured coefficient of thermal expansion of the girder concrete, and the coefficient of thermal expansion of the strain gage wire provided by the manufacturer.  Therefore, the plotted average values in figure 12 represent corrected strains that theoretically do not include effects due to temperature change.

Strain readings taken just prior to release of the strands served as the zero reference for the average concrete strains reported in figure 12.  After strand release, the average compressive strains measured in the bottom flange gradually increased due to the effects of creep and shrinkage until the time when the deck slab was added.  The corresponding measured strains in the top flange essentially mirrored the behavior of the bottom flange until the girders were erected at the job site (between 126 to 134 days after release).

During the time period bounded by the dates of erection and deck casting, the compressive strain in the bottom flange continued to increase while the top flange strains transitioned from slight tension to compression.  The gradual load additions resulting from the diaphragms formwork and deck slab reinforcing steel did not produce noticeable changes in the bottom flange strains.  However, the effects of these additions were clearly evident in the measured top flange strains.  The average data plotted in figure 12 indicate a marked reduction in the bottom flange compressive strain and corresponding increase in the top flange compressive strain occurring 185 days after release, denoting the elastic response due to placement of the deck slab concrete.

The measured concrete strain changes at the center of gravity of the prestressing strands were used to quantify prestress loss parameters caused by elastic shortening, concrete creep, and concrete shrinkage.  Using the compatibility assumption that the changes in concrete strain measured at the center of gravity of the prestressing strands are equal to the corresponding average steel strain changes, the measured values reported in figure 12 can be used to calculate prestress losses using the modulus of elasticity of the strand.

When the bottom flange strain data shown in figure 12 are edited to remove elastic strain effects resulting from external loading and multiplied by the average measured modulus of elasticity of the prestressing strand equal to 27,950 ksi (193 MPa) reported in table 6, the resulting plot of prestress loss shown in figure 13 results.  The data plotted in figure 13 represent the total measured prestress loss in each girder due to the combined effects of elastic shortening, concrete creep, and concrete shrinkage for a time interval beginning at release of the prestressing strands and ending at the conclusion of the one-year monitoring period.

For comparison with the measured data, prestress losses were calculated for a typical interior girder using the provisions of the AASHTO Standard Specifications [5].  Prestress loss calculations were made to evaluate two different scenarios.  The first scenario represents the “as designed” condition, where the calculated loss parameters are based on specified material properties and the assumption that the initial strand stress at time of release equals 69 percent of the 270 ksi (1862 MPa) ultimate stress (as allowed by Article 9.16.2.1.2 of the AASHTO Standard Specifications).  The second scenario represents the “as constructed” condition, where the calculated loss parameters are based on measured material properties and initial strand stress at time of release determined based on data from load cell readings performed during girder fabrication.  Specific conditions associated with the two prestress loss calculation scenarios are given in table 9.

Figure 13
Average prestress loss versus time

Table 9 
Prestress loss calculation scenarios

| Calculation Parameter | Calculation Scenario |
| --- | --- |
|  | As-Designed | As-Constructed |
| Girder concrete f(ci, psi | 6,670 | 9,250 |
| Girder concrete Eci, ksi | 4,950 | 6,000 |
| Girder concrete f(c, psi | 10,000 | 11,260 (56 days) |
| Girder concrete Ec, ksi | 6,062 | 6,300 (56 days) |
| Girder unit weight, pcf | 150 | 146 (56 days) |
| Deck slab f(c, psi | 4,200 | 7,760 (28 days) |
| Deck slab Ec, ksi | 3,929 | 5,650 (28 days) |
| Deck slab unit weight, pcf | 150 | 145 (28 days) |
| Haunch thickness, in. | 2 | 2 |
| Strand stress @ release, ksi | 186,300 | 186,590 |
| Strand modulus of elasticity, ksi | 28,000 | 27,950 |

Measured and calculated prestress losses for the interior HPC girders of Span 43 are given in table 10.  The tabulated prestress losses are presented in terms of the four loss components defined in the AASHTO Standard Specificationsm, namely, elastic shortening, shrinkage, creep, and relaxation [5].  Measured elastic shortening prestress loss was determined based on the average initial concrete strain change resulting from release of the prestress force.  Subsequent increases in the measured concrete compressive strain, exclusive of reductions caused by external load effects, were used to quantify prestress loss due to the combined effects of girder concrete shrinkage and creep.  The measured shrinkage and creep loss components are lumped together in table 10 because it is not possible to distinguish the individual contribution from each effect based on the measured strain change alone. The measured pretress loss due to steel relaxation cannot be discerned from the measured strain data and, therefore, is not included among the measured losses.  However, it should be noted that the relaxation loss component is generally small in comparison with other loss components making up only approximately 1 to 2 percent of the total prestress loss.

Table 10
Measured and calculated prestress losses using AASHTO Standard Specifications

| Prestress Loss Component | Measured Losses, psi | Calculated Losses, psi |
| --- | --- | --- |
|  |  | As-Designed | As-Constructed |
| Elastic Shortening | 19,608 | 19,640 | 16,314 |
| Shrinkage | 8,706 | 5,750 | 5,750 |
| Creep |  | 32,951 | 33,610 |
| Relaxation | — | 1,101 | 1,401 |
| Total | 28,314 | 59,442 | 57,075 |

As indicated by the data in table 10, the measured elastic shortening prestress loss correlated well with the corresponding “as-designed” calculated loss.  Correlation between the measured elastic shortening loss and corresponding “as-constructed” calculated loss was not as favorable.  The calculated elastic shortening loss is dependent on the concrete modulus of elasticity at the time of strand release.  As indicated in table 9, the “as-designed” elastic shortening loss was calculated using an assumed concrete modulus of elasticity value of 4,950 ksi (34 GPa) while the “as-constructed” elastic shortening value was calculated using a measured concrete modulus of elasticity value of 6,000 ksi (41 GPa).  The modulus of elasticity value used in the “as-constructed” elastic shortening loss calculation was measured several hours after the time that release actually took place and, therefore, may have been somewhat greater than the actual concrete modulus of elasticity at the time of strand release.

Another possible explanation for the discrepancy between the measured and “as-constructed” elastic shortening prestress loss could be that the measured concrete strains resulting from release included some creep and shrinkage loss.  The time duration between the pre- and post-release strain readings made for the four instrumented girders was typically about 1.5 hours.  The post-release readings were typically taken within 20 minutes after the conclusion of strand release.  While efforts were made to minimize the elapsed time between the pre- and post-release strain measurements, it is likely that the resulting measured change in strain occurring over this time interval included some creep and shrinkage loss.

As shown in figure 13, the measured prestress loss for each girder gradually increased from the time of strand release until approximately 340 days after release.  From that point, the measured losses decreased slightly over the next 160 days and then began to increase again from approximately 500 days onward until reaching an apparent maximum value approximately 650 days after release.  There are two readily-apparent explanations for the observed fluctuation in measure prestress loss.  One explanation is that the temperature compensation applied to the measured strains is not precise, causing seasonal temperature variations to have a slight yet noticeable effect on the measured prestress loss.  The second explanation relates to shrinkage of the deck slab concrete.  Deck slab shrinkage will tend to reduce bottom flange compressive strains.  Consequently, the measured prestress losses plotted in figure 13 beyond 185 days include increases due to the combined effect of continuing creep and shrinkage of the girder concrete and reductions due the progression of deck slab shrinkage.  Although the measured prestress losses plotted in figure 13 likely include some negating effects due to deck slab shrinkage, the observed fluctuations appear to be more consistent with the seasonal temperature variation causation scenario than the deck slab shrinkage causation scenario.

The total measured prestress loss value reported in table 10 is based on the average of the maximum pretress loss values for each interior girder typically occurring approximately 650 days after release.  As indicated by the data in table 10, the total measured prestress loss is approximately 50 percent less than the corresponding “as-designed” and “as-constructed” calculated total prestress loss values.  The calculated prestress losses should be viewed as ultimate (end of service life) values.  Therefore, total losses measured within the first few years of service would be expected to be less than calculated values.   However, according to PCI’s “Recommendations for Estimating Prestress Losses,” 74 percent of the ultimate creep and 86 percent of the ultimate shrinkage would be expected to have taken place within the first year [9].  Applying these percentages to the calculated creep and shrinkage loss values, total prestress losses equal to 50,070 psi (345 MPa) and 47,531 psi (328 MPa) would be expected after one year of service for the “as-designed” and “as-constructed” scenarios, respectively.  The total measured prestress loss is approximately 40 percent less than the calculated losses that would be expected after one year.  Based on this observation, it is likely that the total final prestress loss measured at the end of service life will also be less than the final calculated loss values reported in table 10.

Based on the data in table 10, it can be concluded that the prestress losses calculated using provisions outlined in the AASHTO Standard Specifications may tend to over-estimate actual losses occurring in service.  However, the measured losses reported in table 10 do not include the initial reduction in strand force measured during girder fabrication.  As indicated in table 8, strand load measurements made during girder fabrication indicated an average of 7.9 percent reduction in prestress force occurring prior to release.  This measured reduction in strand force translates to a prestress loss of 15,945 psi (109 MPa).  As indicated in figure 3, internal concrete temperatures increased rapidly after placing the concrete and remained quite high at the time of strand release.  Based on this observation, it is apparent that a portion of the strand force reduction noted prior to release was likely due to thermal expansion of the strand.  In addition, depending upon when bond is established between the strand and concrete, a portion of this measured loss would likely have been recovered upon subsequent cooling of the concrete.  Nonetheless, the measured reductions in strand force greatly exceeded calculated allowances for steel relaxation and thermal expansion and likely constituted an additional source of significant prestress loss not specifically addressed by existing design provisions nor included in the measured losses reported in table 10.

Measured prestress losses that were considerably less than corresponding design losses calculated using provisions from the AASHTO Standard Specifications have been reported in previous HPC research sponsored by LTRC [1], [2].  Like the instrumented HPC girders in the Rigolets Bridge, measured long-term prestress loss in Girder BT3 from the feasibility evaluation research program was also approximately 50 percent less than the corresponding calculated design value [1].  The average measured prestress loss for the instrumented girders in the Charenton Canal Bridge was approximately 33 percent less than the corresponding calculated design value [2].  The HPC girders in the Rigolets Bridge and Girder BT3 from the feasibility evaluation were made with concrete incorporating approximately 10 percent silica fume by weight of cementitious materials, whereas the Charenton Girders were made using concrete incorporating 30 percent Class C fly ash by weight of cementitious materials.  Therefore, there is evidence to suggest that the use of silica fume may provide a greater benefit we respect to reducing total prestress loss than Class C fly ash.

For further comparison with the measured data, prestress losses were also calculated for a typical interior girder using the latest provisions of the AASHTO LRFD Bridge Design Specifications, 4th Edition (Including 2008 Interims) defined in Sections 5.9.5.2.3 and 5.9.5.3 [10].  Prestress loss calculations were made using the same two scenarios (“as-designed” and “as-constructed”) as used in the previous calculations and reported in table 9.  However, the strand stress at release for the “as-designed” condition was taken as 68 percent of ultimate (initial 10 percent reduction) instead of the 69 percent (initial 8 percent reduction) value cited in the AASHTO Standard Specifications [5].  Measured and calculated prestress losses for the HPC girders of Span 43 are given in table 11.

Table 11
Measured and calculated prestress losses using AASHTO LRFD Bridge Design Specifications

| Prestress Loss Component | Measured Losses, psi | Calculated Losses, psi |
| --- | --- | --- |
|  |  | As-Designed | As-Constructed |
| fpES | 19,608 | 19,092 | 16,304 |
| fpLT | 8,706 | 22,388 | 17,690 |
| Total | 28,314 | 41,480 | 33,994 |

As indicated by the data in table 11, the calculated fpES loss for both the “as-designed” and “as-constructed” conditions was nearly equal to the corresponding calculated elastic shortening loss reported in table 10.  This finding was expected since the equation for fpES cited in the AASHTO LRFD Bridge Design Specifications (Eq. 5.9.5.2.3a-1) is essentially the same as the equation for the elastic shortening prestress loss cited AASHTO Standard Specification (Eq. 9-6).  However, in the commentary to Section 5.9.5.2.3 of the AASHTO LRFD Bridge Design Specifications, an alternate equation for fpES is provided.  When the alternate equation (Eq. C5.9.5.2.3a-1) is used, fpES values equal to 16,817 psi (116 MPa) and 14,692 psi (101 MPa) result for the “as designed” and “as-constructed” scenarios, respectively.  The commentary does not provide details related to the technical basis and background associated with the alternate equation.  However, it is apparent that the alternate equation will generally yield a smaller fpES value than the basic equation.

Time-dependent prestress losses (fpLT ) were calculated using the approximate method defined in Section 5.9.5.3 of the AASHTO LRFD Bridge Design Specifications [10].  The calculated fpLT loss for both the  “as-designed” and “as-constructed” conditions shown in table 11 was considerably more than the average creep and shrinkage loss measured in the interior girders of Span 43 since the time of release.  However, these calculated fpLT loss values are considerably less than the corresponding calculated combined creep, shrinkage and relaxation values shown in table 10 for the AASHTO Standard Specification method.

The total prestress loss predicted using AASHTO LRFD Bridge Design Specification method provided better correlation with the total measured loss data for the interior girders of Span 43 than the total prestress loss predicted using AASHTO Standard Specification method.  As indicated by the data in table 11, the total measured prestress loss is approximately 32 and 17 percent less than the corresponding “as-designed” and “as-constructed” calculated total prestress loss values, respectively.

Girder Deflections

During fabrication, three elevation reference points were embedded along the top flange of each of the four instrumented girders.  These points were embedded at midspan and near both ends to provide a permanent reference for girder defection measurements.  Prior to casting the deck slab, the elevation reference points embedded in the top surface of each girder were extended to the elevation of the finished surface of the deck slab.

Girder defection measurements were made using a standard surveyor’s level and custom rod with smallest measurement divisions of 1/16 in. (1.6 mm).  Deflection measurements were made using the level to sight elevations at each reference point location.  Based on these measurements, the deflection was calculated by subtracting the average elevation of the two girder ends from the midspan elevation.

During construction, girder midspan deflection measurements were made prior to strand release, after strand release, after girder storage, at a concrete age of 28 days, once a month for the next two months, before shipping, after erection, and before and after deck casting.  After casting the deck slab, deflection measurements were made once a week for the first month, once a month for the first three months, and every six months during the one-year monitoring period.  The measured midspan deflection versus time for each of the four instrumented girders is shown in figure 14.

The positive deflection values shown in figure 14 represent a net upward deflection (camber), initiating at the time of prestressing strand release.  The plotted deflection data indicate a marked reduction in camber occurring approximately 185 days after release denoting the elastic response due to placement of the deck slab concrete.

Figure 14
Measured midspan deflection versus time

Average measured deflections and corresponding calculated deflections are given in table 12 for various stages of construction.  The tabulated calculated deflection values are for a typical interior girder, and included both the “as design” and “as constructed” scenarios previously used for the prestress loss calculations.  Deflection calculations were carried out using a traditional moment-area approach along with girder and deck slab properties shown in table 9.  As indicated by the data in table 12, the initial average measured camber at release was less than the corresponding “as-design” calculated value, but correlated well with the “as-constructed” calculated value.

The measured deflection values reported in table 12 for the “girder storage” stage were taken approximately seven days after release.  As indicated by the data reported in table 12, the measured deflections taken after the girders were moved into storage were approximately 50 percent greater than the measured values taken immediately after strand release.  The reported increase in measured camber was likely due to an increase in prestress force due to concrete cooling and moving the girders off of the casting bed, a decrease in self-weight deflection due to concrete modulus of elasticity increase, and camber growth effects caused by concrete creep and shrinkage deformations.

Table 12
Measured and calculated girder deflections

| Time After Release, days | Construction Stage | Measured Deflection, in | Calculated Deflection, in. |
| --- | --- | --- | --- |
|  |  | Range | Average | As-Designed | As-Constructed |
| 0.01 | After releasea | 2.16-2.44 | 2.26 | 2.92 | 2.39 |
| 6-7 | Girder storageb | 3.13-3.48 | 3.31 | 3.13 | 2.45 |
| 110-118 | Before shipment | 3.23-3.73 | 3.54 | 3.26 | 2.48 |
| 110-118 | Before shipment, with PCI multipliers | ____ | ____ | 5.80 | 4.40 |
| 177-185 | Before deck cast | 2.42-3.64 | 2.90 | 3.26 | 2.48 |
| 177-185 | After deck cast | 1.23-2.39 | 1.67 | 1.58 | 0.91 |
| 426-434 | Final reading | 1.09-2.39 | 1.64 | 1.58 | 0.91 |
| 426-434 | Final reading, with PCI multipliers | ____ | ____ | 2.62 | 1.06 |

a 	Calculated deflection values for the release stage were based on a span equal to the full 130.8-ft end-to-end length of the girder.  Calculated values for all other stages were based on the design center-to center distance between bearing supports equal to 129.8 ft.

b	Calculated deflection values for the storage stage were based on a girder concrete modulus of elasticity equal to the average of the corresponding Eci and Ec values shown in table 9.  All other subsequent calculated values are based on the corresponding Ec values shown in table 9.

As indicated by the data for the “girder storage” construction stage in table 12, the calculated deflection for the “as-design” condition was in closer agreement with measured values than the calculated deflection for the “as-constructed” condition.  As previously noted, the opposite was true for the initial release values.   However, it should be noted that none of the calculated deflection values reported in table 12, except for those including PCI multipliers, account for pretress losses or camber growth effects caused by concrete creep and shrinkage deformations.

Two sets of deflection values are reported in table 12 for the “before shipment” stage: one where the calculated values are presented without modification and another where the calculated values have been modified using applicable long-term multipliers defined in table 4.8.4.1 of the PCI Design Handbook [11].   As indicated by the data reported in table 12, application of the PCI multipliers for the “at erection” condition to the calculated deflections for the “before shipment” construction stage resulted in overestimation of the actual measured camber deflection.  Although still used within the bridge design community, the long-term multipliers defined in the PCI Design Handbook are not specifically stipulated as being suitable for estimating deflections in long-spanning bridge girders or other prestressed members with span-to-depth ratios exceeding 20.  The span-to-depth ratio for the BT-78 HPC girders fabricated for the Rigolets Pass Bridge is approximately 20.  Based on the measured and calculated deflection data reported in table 12 for the “before shipment” construction stage, it is concluded that the PCI multipliers used to predict girder deflections at time of erection may tend to overestimate deflections in bridge girders with span-to- depth ratios at the upper limit of the recommended range cited in Section 2.2.2 of the PCI Design Handbook [11].

Based on the data reported in table 12, the average measured change in camber deflection among the four instrumented girders resulting from addition of the deck slab was 1.23 in. (31 mm).  The corresponding calculated change in camber deflection for both the “as-design” and “as-constructed” conditions was 1.68 in. (43 mm) and 1.57 in. (40 mm), respectively.  The average measured value is less than both of the corresponding calculated deflection values.  It is interesting to note that the measured change is bottom flange strain due to the addition of the deck slab shown in figure 12; it was also less than what would be expected based on traditional elastic analysis.  Two likely explanations for this lack of correlation are (1) the influence of dead load contribution from reinforcing steel and formwork on the “before cast” readings, and (2) the influence of deck slab concrete temperature increase on the “after cast” readings.  The “before cast” readings were taken after all of the formwork and deck reinforcing steel were in place.  Consequently, these readings already included a portion of the deck slab dead load.  The “after cast” readings were taken after the deck slab concrete had achieved initial set and had begun to generate heat from hydration.  During the time period between the “before cast” and “after cast” readings, the temperature of the girder top flange concrete increased by approximately 10 ºF (6 ºC) due to hydration of the adjacent deck slab concrete.   This temperature increase will tend to cause an increase in compressive strain in the bottom flange and a corresponding decrease in the net measured downward deflection resulting from the addition of the deck slab concrete.

Two sets of deflection values are reported in table 12 for the “final” stage: one where the calculated values are presented without modification and another where the calculated values have been modified using applicable long-term multipliers defined in table 4.8.4.1 of the PCI Design Handbook [11].   As indicated by the data reported in table 12, the calculated deflection for the “as-design” condition was in closer agreement with measured values than the calculated deflection for the “as-constructed” condition.  However, it should be noted that calculated final deflection values reported in table 12 (without the PCI multipliers) do not  account for the effects of pretress losses resulting for girder concrete creep and shrinkage deformations or effects of shrinkage of the deck slab concrete.  The plot shown in figure 14 indicates a slight but gradual increase in girder midspan camber with time.  This subtle increase likely indicates the net effect of these phenomena with the girder creep and shrinkage outweighing the effect of deck slab shrinkage by a narrow margin.

Application of the PCI multipliers to the calculated deflections for the “final” construction stage resulted in overestimation of the actual measured camber deflection for the “as-designed” condition and an underestimation of the actual measured camber deflection for the “as-constructed” condition.  Based on these observations, no specific conclusions may be drawn regarding applicability of the PCI multipliers used to predict final girder deflections.

Deck Strains

Concrete strains at mid-depth of the deck slab were measured at seven transverse locations at mid-length of Span 43.  Four of the seven strain gages (S1, S3, S5, and S7) were located directly above the centerline of Girders 43A, 43B, 43C, and 43D.  The remaining three strain gages (S2, S4, and S6) were located midway between girders 43A, 43B, 43B, 43C, and 43D.  The lead wire for the gage situated above Girder 43A (S1) was damaged beyond repair during removal of the deck slab side forms.  Consequently, no data from this gage could be obtained.  A plot of concrete strain versus time for the remaining six gages is shown in figure 15.

As indicated by the data shown in figure 15, the measured strains from gages installed directly above the girders (S3, S5, and S7) exhibited similar behavior while the remaining three gages (S2, S4, and S6) exhibited somewhat variable behavior.  All six gages exhibited a trend of initial compression (presumably due to initial drying shrinkage) followed by a gradual transition to increasing tension.  This trend of increasing tension is likely due to the effects of girder creep and shrinkage deformations and is consistent with the trends seen in the measured girder strains (figure 12) and the measured girder deflections (figure 14).  The abrupt increase in deck slab compressive strain occurring at approximately 260 days after concrete placement was likely due to the addition of the barrier railing installed along both sides of the span.

Figure 15
Deck slab concrete strain versus time

Seasonal Temperature and Strain Fluctuations

Each of the vibrating wire strain gages installed in the girders and deck slab of Span 43 were connected to an on-site data acquisition system (DAS) with remote access and data collection capabilities.  In addition to the vibrating wire strain gages, an external temperature and humidity probe was connected to the DAS for the purpose of monitoring ambient conditions at the bridge site.  The DAS was programmed to read and store measured data from each gage once per hour over a one-year monitoring period.  The data recorded by the DAS was used to evaluate daily and seasonal fluctuations in both concrete temperatures and strains.

DAS monitoring of Span 43 commenced on January 11, 2008, which was a few days before the bridge was opened to traffic.  Seasonal fluctuations in concrete temperatures and strains were evaluated by examining and comparing the measured hourly data for consecutive days of a typical winter or summer month to represent a range of different weather conditions.

Winter Temperature and Strain Data

Typical winter season fluctuations in measured concrete temperatures and strains were evaluated by examining data recorded during the month of February 2008.  As expected, average internal concrete temperatures measured in both the girders and deck slab generally followed the corresponding trend of the outside ambient temperature.  However, as indicated by the black and blue plot lines shown in figure 16, the average internal girder temperatures tended to lag behind the ambient temperature (thick, light-blue line) whenever substantial increases or decreases occurred over a short time period. The average daily high deck slab temperatures tended to slightly exceed the corresponding ambient temperatures on days with minimal cloud cover during afternoon hours as indicated by the red plot line in figure 16.

Figure 16
Measured concrete temperature data – February 2008

The temperature-sensing element of the vibrating wire strain gage located in the bottom flange of exterior Girder 43D on the south side (gage 43D-BF-1) also registered concrete temperatures that exceeded the corresponding ambient temperature as indicated by the green plot line in figure 16.  During the winter months, the sun is at a greater angle relative to the south side surface of Girder 43D than to the horizontal surface of the deck slab.  Consequently, the south side of Girder 43D receives more solar radiation than the deck slab during a typical sunny winter day and will tend to register higher concrete temperature readings.  As indicated in figure 16, the internal concrete temperature near the south side surface of Girder 43D was as much as 15 °F greater than the corresponding ambient temperature on some days.

Average internal concrete strains measured in both the girders and deck slab generally exhibited daily fluctuations due to changes in ambient conditions.  As indicated by the black and red plot lines shown in figure 17, the average daily concrete strain changes in the bottom flange and deck slab were relatively small, ranging from approximately 0 to 50 millionths.  The average daily concrete strain change in the top flange (depicted by the blue plot line in figure 17) was typically larger and more consistent than that noted in the bottom flange and deck slab, ranging from approximately 50 to 100 millionths.

The vibrating wire strain gage located in the bottom flange of exterior Girder 43D on the south side (gage 43D-BF-1) also registered daily concrete strain fluctuations of as much as 100 millionths as indicated by the green plot line in figure 17.  These strain fluctuations appear to follow the same trend as the concrete temperature fluctuations shown in figure 16 and were likely accentuated by the effect of increased solar radiation on the southern bridge exposure throughout the year.

The daily strain fluctuations shown in figure 17 for the month of February are driven by changes in weather conditions at the bridge site (temperature, cloud cover, precipitation, relative humidity, etc.).  Although not sustained for prolonged periods of time, these fluctuations will still have a temporary superimposed effect on both girder and deck slab concrete stress levels.  Based on the measured 56-day girder concrete modulus of elasticity of 6,288 ksi (43.35 GPa), a change in strain of 100 millionths would produce a corresponding stress change equal to approximately 628 psi.  Consequently, it is apparent that changing weather conditions at the bridge site can have a significant effect on in-service stress levels in both the girders and deck slab.

Figure 17
Measured concrete strain data – February 2008

Summer Temperature and Strain Data

Typical summer season fluctuations in measured concrete temperatures and strains were evaluated by examining data recorded during the month of August 2008.  As previously noted for the winter data, average internal concrete temperatures measured in both the girders and deck slab generally followed the corresponding trend of the outside ambient temperature. However, as indicated by the black plot line shown in figure 18, the average girder bottom flange internal concrete temperatures tended to lag behind the ambient temperature (thick, light-blue line) whenever substantial increases or decreases occurred over a short time period. The average daily high deck slab and girder top flange temperatures tended to exceed the corresponding ambient temperatures on days with minimal cloud cover during afternoon hours as indicated by the red plot line in figure 18.

The temperature-sensing element of the vibrating wire strain gage located in the bottom flange of exterior Girder 43D on the south side (gage 43D-BF-1) also registered concrete temperatures that exceeded the corresponding ambient temperature as indicated by the green plot line in figure 18.  During the summer months, the sun is at a greater angle relative to the horizontal surface of the deck slab than to the south side surface of Girder 43D.  Consequently, the deck slab receives more solar radiation than the south side of Girder 43D during a typical sunny summer day and will tend to registered higher concrete temperature readings.  As indicated in figure 18, the average deck slab temperature was as much as 15 °F greater than the corresponding ambient temperature on some days.

Figure 18
Measured concrete temperature data – August 2008

Average internal concrete strains measured in both the girders and deck slab generally exhibited daily fluctuations due to changes in ambient conditions.  As indicated by the black and red plot lines shown in figure 19, the average daily concrete strain changes in the bottom flange and deck slab were relatively small, ranging from approximately 0 to 70 millionths.  The average daily concrete strain change in the top flange (depicted by the blue plot line in figure 19) was typically larger and more consistent than that noted in the bottom flange and deck slab, ranging from approximately 50 to 100 millionths.  The recorded average strain data shown in figure 19 for typical summer exposure conditions were similar to those shown in figure 16 for typical winter exposure conditions.  However, average daily measured strain fluctuations in the girder bottom flange and deck slab were noticeably more pronounced for winter exposure than for summer exposure.

Figure 19
Measured concrete strain data – August 2008

The vibrating wire strain gage located in the bottom flange of exterior Girder 43D on the south side (gage 43D-BF-1) registered daily concrete strain fluctuations of as much as 80 millionths as indicated by the green plot line in figure 19.  These strain fluctuations appear to follow the same trend as the concrete temperature fluctuations shown in figure 18 and were likely accentuated by the effect of increased solar radiation on the southern bridge exposure throughout the year.

The daily strain fluctuations shown in figure 19 for the month of August are driven by changes in weather conditions at the bridge site (temperature, cloud cover, precipitation, relative humidity, etc.).  Although not sustained for prolonged periods of time, these fluctuations will still have a temporary superimposed effect on both girder and deck slab concrete stress levels.  Based on the measured 56-day girder concrete modulus of elasticity of 6,288 ksi (43.35 GPa), a change in strain of 100 millionths would produce a corresponding stress change equal to approximately 628 psi.  Consequently, it is apparent that changing weather conditions at the bridge site can have a significant effect on in-service stress levels in both the girders and deck slab.

# CONCLUSIONS

Design and construction of the Rigolets Pass Bridge has demonstrated yet again that a bridge using HPC can be successfully constructed in Louisiana using locally available materials.  Specific conclusions from various aspects of the research are as follows:

- The specified concrete compressive strength for the HPC girders was 6,670 psi at release and 10,000 psi (69 MPa) at 56 days.  The measured concrete compressive strengths for the four instrumented girders exceeded the specified strength at both the release and 56-day test ages.

- The AASHTO Standard Specification equation for modulus of elasticity provided a conservative prediction of the actual measured girder concrete modulus of elasticity obtained from this research.  However, based on data from other previous HPC research sponsored by LTRC, use of modulus of elasticity values that are slightly less than those predicted by the AASHTO expression may be warranted when design concrete compressive strengths exceed 10,000 psi (69 MPa).

- The AASHTO Standard Specification equation for modulus of rupture provided a conservative prediction of the actual measured girder concrete modulus of rupture obtained from this research.  Based on data from this research and other previous HPC research sponsored by LTRC, use of k factors greater than the 7.5 value currently incorporated in the AASHTO Standard does not appear warranted.

- The average measured chloride permeability of the girder concrete obtained from this research (151 coulombs) was considerably less than the 2,000 coulomb limit stipulated in the project specifications.  Based on the measured chloride permeability data generated from this research and from the Charenton Canal Bridge research, it appears that the use of silica fume provides a much greater benefit relative to reducing overall permeability than Class C fly ash.

- According to the ACI Committee 209 Report (ACI 209R-92), the ultimate creep coefficient of concrete normally falls in the range of 1.30 to 4.15, and ultimate shrinkage will normally fall into the range of 415 to 1070 millionths [7].  The creep coefficient after one year reflected by the measure test data fell approximately in the middle of the expected range.  The measured shrinkage after one year fell well below the expected range. Based on these data, lower-than-normal measured girder prestress losses due to the combined effects of creep and shrinkage would be expected.

- The specified concrete compressive strength for the deck slab concrete was 4,200 psi (29 MPa) at 28 days.  The measured concrete compressive strengths for all test ages (7, 28, and 56 days) exceeded the specified strength.

- The average measured chloride permeability of the deck slab concrete obtained from this research (1,028 coulombs) was less than the 2,000 coulomb limit stipulated in the specifications for the Rigolets Pass Bridge project.

- Force levels measured in selected prestressing strands made just prior to release were approximately 8 percent less than the specified initial force level.  Approximately half of this reduction in prestress force was evident immediately after stressing all of the strands.  The balance of the reduction was likely caused by thermal expansion due to the heat generated by the concrete during initial curing.

- Total average measured prestress loss for the four instrumented HPC girders was approximately 50 percent less than corresponding final values calculated using the provisions of the AASHTO Standard Specifications.  Based on the measured long-term prestress loss data from this research, and from previous LTRC-sponsored HPC research, there is evidence to suggest that the use of silica fume in the bridge girder concrete may provide a greater benefit with respect to reducing total prestress loss than Class C fly ash.

- Prestress losses predicted using provisions of the AASHTO LRFD Bridge Design Specification provided better correlation with the total measured prestress loss for Span 43 of the Rigolets Pass Bridge than the losses predicted using provisions of the AASHTO Standard Specifications.

- Based on comparisons between the measured and corresponding calculated values, it is concluded that application of PCI multipliers for the “at erection” stage may tend to overestimate long-term deflections in bridge girders with span-to depth ratios at the upper limit of the recommended range cited in Section 2.2.2 of the PCI Design Handbook.  Based on available data, it appears that application of the PCI multipliers for the “final” stage will provide better correlation with corresponding measured values than the “at erection” multipliers.

- The measured deck strains exhibited a trend of initial compression (presumably due to initial drying shrinkage) followed by a gradual transition to increasing tension (likely due to the effects of girder creep and shrinkage deformations).  Trends observed in the measured deck strains were consistent with corresponding trends observed in measured girder concrete strains and deflections.

- Based on the measured trends and fluctuations observed during typical winter and summer exposure conditions, it is apparent that changing weather conditions at the bridge site can have a significant effect on in-service stress levels in both the girders and deck slab.

RECOMMENDATIONS

Based on the Discussion of Results and Conclusions reported herein, the following recommendations are offered for consideration:

- The LADOTD should continue implementing HPC with specified compressive strengths up to 10,000 psi on all bridges where its use is beneficial and economical.

- The LADOTD should continue to use the existing AASTHO equations for modulus of elasticity and modulus of rupture when the design girder concrete compressive strength is 10,000 psi (69 MPa) or less.  When the design girder concrete compressive strength exceeds 10,000 psi (60 MPa), the use of a slightly reduced value for the modulus of elasticity would be appropriate.

- The use of HPC incorporating 10 percent silica fume by weight of cementitious materials should be considered whenever extremely low permeability or minimization of prestress loss is desirable or required.

- The PCI multipliers should not be relied on to predict long-term camber or deflections in HPC bridge girders.

The LADOTD should continue implementation of parallel research programs similar to this program on projects where HPC is specified in order to continue expansion of the existing material and performance database.

# ACRONYMS, ABBREVIATIONS, AND SYMBOLS

AASHTO	American Association of State Highway and Transportation Officials

ASTM		American Society for Testing and Materials

BT		bulb tee

ºC		degrees Celsius

cu		cubic

DAS		data acquisition system

Ec		concrete modulus of elasticity

ºF		degrees Fahrenheit

fl oz		fluid ounce

ft.		foot / feet

f(c		specified compressive strength of concrete

GCP		Gulf Coast Pre-Stress, Inc.

HPC		high performance concrete

In.		inch(es)

kg		kilogram

kN		kilonewton

ksi		kip per square inch

LADOTD	Louisiana Department of Transportation and Development

L		liter(s)

LRFD		Load and Resistance Factor Design

Lb.		pound(s)

MOR		modulus of rupture

MPa		megapascal

m		meter(s)

mm		millimeter(s)

N		newton

No.		number

PCI		Precast/Prestressed Concrete Institute

pp.		pages

psi		pounds per square inch

sq		square

wc		unit weight of concrete

yd		yard

c		concrete coefficient of thermal expansion

@		at

# REFERENCES

- Bruce, R. N.; Russell, H. G.; Roller, J. J.; and Martin, B. T., “Feasibility Evaluation of Utilizing High Strength Concrete in Design and Construction of Highway Bridge Structures,” Final Report – Louisiana Transportation Research Center, Research Report No. FHWA/LA-94-282, Baton Rouge, LA, 1994, 168 pp.

- Bruce, R. N.; Russell, H. G.; Roller, J. J.; and Hassett, B. M., “Implementation of High Performance Concrete in Louisiana Bridges,” Final Report – Louisiana Transportation Research Center, Research Report No. 310, Baton Rouge, LA, 2001, 67 pp.

- Bruce, R. N.; Russell, H. G.; and Roller, J. J., “Fatigue and Shear Behavior of HPC Bulb-Tee Girders,” Interim Report – Louisiana Transportation Research Center, Research Report No. FHWA/LA. 03/382, Baton Rouge, LA, 2003, 57 pp.

- Bruce, R. N.; Russell, H. G.; and Roller, J. J., “Fatigue and Shear Behavior of HPC Bulb-Tee Girders,” Final Report – Louisiana Transportation Research Center, Research Report No. FHWA/LA. 05/395, Baton Rouge, LA, 2005, 59 pp.

- Standard Specifications for Highway Bridges, Sixteenth Edition, American Association of State Highway and Transportation Officials, Washington, DC, 1996.

- Louisiana Standard Specifications for Roads and Bridges, State of Louisiana, Department of Transportation and Development, Baton Rouge, LA, 2006, 895 pp.

- ACI Committee 209, “Prediction of Creep, Shrinkage and Temperature Effects in Concrete Structures,” (ACI 209R-92) (Reapproved 1997), American Concrete Institute, Detroit, 1992, 47 pp.

- PCI Plant Certification Committee, “Manual for Quality Control for Plants and Production of Structural Precast Concrete Products,” MNL-116-99, Precast, Prestressed Concrete Institute, Chicago, IL, 1999.

- PCI Committee on Prestress Losses, “Recommendations for Estimating Prestress Losses,” PCI Journal, Vol. 20, No. 4, July-August 1975, pp.44-75.

- AASHTO LRFD Bridge Design Specifications, Fourth Edition (Including 2008 Interim), American Association of State Highway and Transportation Officials, Washington, DC, 2007.

- PCI Industry Handbook Committee, “PCI Design Handbook, Sixth Edition,” MNL 120-04, Precast, Prestressed Concrete Institute, Chicago, IL, 2004.

# Text boxes

Technical Report Documentation Page

45’-11”

12’-7”

12’-7”

12’-7”

4’-1”

4’-1”

8-in. thick

deck slab

Girder A

Girder B

Girder C

Girder D

BT-78 girder (typ.)

Reinforced concrete diaphragm

@ span 1/3 points (typ.)

Barrier railing (typ.)

N

Seven-wire strand

instrumented with

load cell (typ.)

7.5 in.

Centroid of strand group

Vibrating wire strain gages

embedded in lower flange

Vibrating wire strain gages

embedded in upper flange

Deck slab vibrating wire strain gages installed over each girder

and mid-way between each girder

Deck slab vibrating wire strain

gages installed over each girder

and mid-way between each girder